## Slide 1
Hrvatsko asfaltersko društvo
Proizvodnja i tehnologije asfalta s dodatkom recikliranog asfalta i niskotemperaturni asfalti
Jürg Moser
Seminar ASFALTNI KOLNICI 2015
Opatija, 05. – 06. 03. 2015.

## Slide 2: Asphalt recycling
www.ammann-group.com

## Slide 3: Intact Living Space
We all want an efficient road network. And we all need our nature.
Notes: Die Produzenten von Asphalt tragen eine große Verantwortung. Ammann trägt diese Verantwortung mit.
Lebensraum und Mobilität in Einklang bringen.

## Slide 4: Road Construction Evolution
Villages
Local connections
Cities, ports
National connections
Fast and save
connections
Ecological connections
Green Road
Highways
Paved Roads
Unpaved Ways
Topic of our generation

## Slide 5: Modern Plants reduce CO2 Emissions
Moisture reduction
Lower temperatures (WAM Foam)
Credits for recycling
More efficient burner and dryer
Optimized insulation and electrical system
Industry Average
Improved Plant
-45 % of the CO2 emissions
Notes: Q1-4 New age plants reduce the CO2 emission 10%, 45% 90%?
Q1-5 Name 3 different ways to reduce CO2
Notes:
Different ways to reduce CO2 emissions

## Slide 6: Modern Plants run with lower operating costs
Recycling
Lower energy consumption
Industry Average
Improved Plant
-35 % of the running costs
Notes: Notes:
Lower CO2 emissions lower costs

## Slide 7: Ecological = Economical
High energy consumption
High emission level
High running costs
Industry Average
Low energy consumption
Low emission level
Low running costs
Improved Modern Asphalt Plant
Notes: Notes:
Different plant levels for different requirements

## Slide 8: Road Construction - Keeping the Asphalt in the Road
Notes: The goal is to keep the ball in the air! Keep the asphalt in the road!
AC 0/11
RA (0/11) 91,5%
Aggregate (8/11) 8%
Störbit 0,5%
Mix temperature 160°C

## Slide 9: Asphalt Recycling Opens Up Huge Potentials
Potentials
Reducing CO2 emissions
Conservation of resources
Reducing costs
Success Factors
Regulatory acceptance
Ensuring quality of reclaimed asphalt
Using up-to-date technologies

## Slide 10: Various Methods of Asphalt Recycling
Continous Quality
very challenginge
In-Place Recycling
Substitutes Sub-base
Materials
Storage
Crushing
Landfill
New Material
Milling

## Slide 11: Alowed Content of Recalimed Asphalt
Country | Wearing Course | Binder Course | Base Course
Belgium | 25% | 50% | 
Denmark | 30% |  | 100%
France | 40% |  | 
Germany | 50% |  | 100%
Hungary | 10% | 20% | 
Ireland | 10% | 50% | 
Poland | 20% | 30% | 
Portugal | 10% | 50% | 
Spain | - | 10-50% | 
Sweden | 20% | 30% | 
Switzerland | 30%* | 30% | 60%
*: Depending on traffic load

## Slide 12: True Recycling = Future of Asphalt
Asphalt Layers
Gravel Layers
Basement (incl. Installations)
30 cm
Down-Cycling
True Recycling

## Slide 13: Joint Efforts to bring Innovation into Reality
National and state road authorities
Support new technologies
Road construction companies
Investing in new technologies
Equipment Manufacturers
Developing new technologies

## Slide 14: Asphalt Recycling – Material Handling
www.ammann-group.com

## Slide 15: Requirements for High Rates of RA Addition
The prerequisites for this are
careful sourcing,
effective receiving inspection,
separate storage,
extensive initial type tests and
machine- and process-specific requirements to be met by the mixing plant.
DAV, 2011

## Slide 16: Waste of Asphalt Next Due To Start-Up and Shut-Down
Undefined and inhomogeneous
mixture of aggregates and bitumen.
Cannot be used for high quality asphalt

## Slide 17: Processing and Handling of RA Material
17
Bitumen 4,0 % Filler 10,6 % Sand 45,8 % > 2 mm 43,6 %
RA 0/22
Bitumen 3,6 % Filler 6,9 % Sand 24,7 % > 2 mm 68,4 %
Bitumen 5,1 % Filler 12,4 % Sand 52,5 % > 2 mm 35,1 %
RA 0/22
RA 0/8
RA 8/22
Screening
Notes: 17

## Slide 18: Processing and Handling of RA Material
18
0/8
8/16
16/32
Notes: 18
Installation in Gardelegen

## Slide 19: Cost Benefits
as1 Auftragsverwaltungs- und Dispositionssysteme
Homogenous stockpile
Production: 600‘000 t per year
RA: 300‘000 t per year
= 50% RA = -38% Raw Material Costs
Grain size-sorted reclaimed asphalt

## Slide 20: Typical Asphalt Recipe
Base course

## Slide 21: Reclaimed Asphalt + Fresh Bitumen
+
=
+
Twin-shaft mixer
Reclaimed asphalt
Fresh bitumen
+
=
Double-coated grains
Homegenous
mastic

## Slide 22: Action Force Mixer For Homogeneity of the Mastic
Batch asphalt production
Continuous asphalt production

## Slide 23: RAP-Feeder
RAP feeder designed to fit the purpose

## Slide 24: Roofing for Deposits and Cold Feeders
as1 Auftragsverwaltungs- und Dispositionssysteme
Aggregate 59%
Exhaust gases 9%
Thermal losses 2%
Moisture 30%
-1% Moisture = +10% Fuel Saving!
Energy inputs for heating and drying of RA material
(Calculation base: 3% moisture, 165°C)

## Slide 25: Roofing for Deposits and Cold Feeders
as1 Auftragsverwaltungs- und Dispositionssysteme

## Slide 26: Storage: well separated recycling material fractions
roofed storage boxes for milled RA from the top asphalt road layers
covered stockpile for crushed RA

## Slide 27: CO2 Reduction through Smart Stockpiles and Loading
6 %
4 %
Moisture
0.5 – 1.0% less moisture:
0.3 – 0.7 kg less heating oil
per tonne

## Slide 28: Asphalt Recycling – Plant Technologies
www.ammann-group.com

## Slide 29: Typical Batch Process
Mineral
Füller
Bitumen
Mischen
Entleeren
0 10 20 30 40 50 60 70
Discontinuous Production

## Slide 30: Different Techniques To Keep the Asphalt in the Road
0%
30%
50%
75%
100%
in elevator
in pug mill
in drying drum
parallel drum
dedicated counter flow drum
Possible Ratio of Reclaimed Asphalt

## Slide 31: RA Cold Addition via Hot Elevator
as1 Auftragsverwaltungs- und Dispositionssysteme
RA cold addition via hot elevator for up to 15%
- Simple, cost efficient installation
- Suitable for bypass operation only
Limits:
Clogging in hot elevator and hot mineral bins

## Slide 32: RAC – Cold RA (directly into mixer)
210°C
30% RA @ 3% H2O
Notes: + The hot aggregate is cooled down by the RA material before adding the binder, thus the added bitumen is not in touch with the very hot mineral aggregate (conventional mixing cycle).
+ The binder contained in the RA material partially covers the virgin aggregate.
- The conventional mixing cycle is longer than the progressive mixing cycle.
- The added binder is not fully available for the fresh aggregate. The binder/filler ration is inaccurate and therefore the stiffening effect reduced. Partially the filler adheres to the RA material which already contains filler.

## Slide 33: Cold recycling in Mixer
Aggregate
Recycling
Steam
Filler
Bitumen
Mixing
Discharge
0 10 20 30 40 50 60 70

## Slide 34: RAC – Cold RA (directly into mixer)
210°C
Aggregate
RA
Evaporation
Filler
Bitumen
Mixing
Emptying
0 10 20 30 40 50 60 70
Aggregate
RA
Evaporation
Filler
Bitumen
Mixing
Emptying
0 10 20 30 40 50 60 70
„conventional“ mixing cycle
„progressive“ mixing cycle
30% RA @ 3% H2O
Notes: + The hot aggregate is cooled down by the RA material before adding the binder, thus the added bitumen is not in touch with the very hot mineral aggregate (conventional mixing cycle).
+ The binder contained in the RA material partially covers the virgin aggregate.
- The conventional mixing cycle is longer than the progressive mixing cycle.
- The added binder is not fully available for the fresh aggregate. The binder/filler ration is inaccurate and therefore the stiffening effect reduced. Partially the filler adheres to the RA material which already contains filler.

## Slide 35: RAC – Coold RA (directly into mixer)
1
2
3
4
5
6
7
8
10
15
20
25
30
35
40
RA feed rate [%]
Design point
MC [%]
0

## Slide 36: Cold Recycling, up to 30% recycling material
Bucket elevator
Puffer silo
Weighing scale
Steam evacuation from mixer
100
0

## Slide 37: RAC Feeding and dosing in Mixer
Bucket elevator and steam evacuation Belt weighing unit

## Slide 38: Ammann RAH50 Drum
RA addition into aggregate drum for addition rates of 40-50%
Tangential RA- material feed
Aggregate feed
New design from Ammann , due to great demand in southern Europe markets
High RA addition rates with low-cost installation
Suitable for bypass-operation only

## Slide 39: Cold recycling via Ring in Drum
Aggregate
Recycling
Filler
Bitumen
Mixing
Discharge
0 10 20 30 40 50 60 70

## Slide 40: Operation of the dryer
MIX enters in a special anular chamber where it continues to increase the temperature in a gentle way up to output without being affected by high flame temperature

## Slide 41
CB 150 with RAH50/2080

## Slide 42
Retrofit in Italy of RAH50/25100

## Slide 43
60% RA @ 3% H2O
RAH – Hot Recycling

## Slide 44
Aggregate
Recycling
Filler
Bitumen
Mixing
Discharge
0 10 20 30 40 50 60 70
Warm recycling via prallel drum

## Slide 45
0
100
200
300
400
500
600
700
800
900
°C
RAP
Gas
Principle of parallel flow

## Slide 46
Hot Recycling, up to 60% Recycling material
Recycling drum
Recycling silo
Bucket elevator
Weighing scale
100

## Slide 47: Recycling Drums (Parallel flow)
270°C

## Slide 48: Recycling Drums (Parallel flow)

## Slide 49: Recycling Drums (Parallel flow)

## Slide 50: Recycling Drums (Parallel flow)

## Slide 51: 100% Recycling Device
Process air heater
RAP dryer
Process air circulation

## Slide 52: 100% Recycling Device (protected)
Combustion chamber
Dryer- and Heating Drum (turning)
Fresh air
Gas mixing
Filter
recirculated, hot air
Low ageing of bitumen
No radiation heat
Low oxygen content
High efficiency
Counterflow dryer
Air recirculation
Low emissions (VOC)
Indirectly heated recycling drum
Recycling-Asphalt
Hot Recycling-Asphalt: 165 °C

## Slide 53: as1 Dynamic RA addition – RAP usage made easy
Benefit
Continuous change of RAP ratio during production process by slider
One recipe is sufficient for various RAP ratios
Integrated wizard for guiding through the recipe input process
… easy RAP ratio change during the ongoing production process
„as1 Dynamic RA addition is one of the best developments by Ammann.“
Helmut Gaal, Plant manager MSO Mischanlagen GmbH
Notes: This module does not require additional Hardware. It is based on RAP analysis from the laboratory.
RAP addition into the mixer only is supported by this module.

## Slide 54: as1 Dynamic RA addition – arguments
Thanks to as1 dynamic RA addition, you get one continuous protocol.
Thanks to as1 dynamic RA addition, Temperature is under control.
Thanks to as1 dynamic RA addition, you get one continuous protocol.
Chart: Dynamic RAP - Temperature control
"RA %" | 5.3025 | 4.8381 | 5.3397 | 5.3883 | 5.3685 | 5.4251 | 5.412 | 5.616 | 10.4608 | 10.2772 | 15.2891 | 15.8517 | 15.7047
"Mix temp" | 171.0991 | 184.2448 | 184.5026 | 188.1112 | 190.1621 | 189.6914 | 188.2905 | 187.4948 | 178.7646 | 179.2914 | 171.4465 | 169.306 | 172.1974
Notes: Based on an estimated Bitumen price of ~ 600 $/ t of Bitumen (2013). (Bitumen reduction depending on remaining bitumen content in the rap), more RAP means as well higher virgin mineral temperatures.
Thanks to RAD higher recycling rates are produced
Thanks to RAD mix temperatures are more stable which equals higher quality
Thanks to RAD you get a continuous mix documentation instead of multiple productions from different recipes.

## Slide 55: Productivity Partnership for a Lifetime
www.ammann-group.com
Thank you for your attention!