## Slide 1: HRvatsko asfaltersko društvo Cold In situ recycling and very thin asphalt concrete - French technology JP Michaut Seminar ASFALTNI KOLNICI 2015 Opatija, 05. – 06. 03. 2015

## Slide 2: Novacol cold in situ recycling
NOVACOL from 1986
More than 25 years
More than 6,000,000m²
In different countries

## Slide 3: What is the cold in-situ recycling?
Cold in-situ recycling consists:
milling or crushing the old pavement up to 20 cm depth,
incorporate in the same time in the milled and crushed material a bituminous emulsion,
In order to stabilize the recycled layer and to give it rejuvenation and cohesion.
The mixture is laid and compacted to constitute a new binder course

## Slide 4: Cold in-situ recycling workshop
PAVER
WINDROW ELEVATORTACK COAT
MIXER MILLING MACHINE
SUPPLY TANKER
E COMPACTOR
ROLLER
(Rejuvenating emulsion)
Length around 200 m only !!!

## Slide 5: Novacol Cold in-situ recycling
PRINCIPLE

## Slide 6: Cold in-situ recycling Objectives and fields
To recycle the upper bituminous layers damaged by fatigue to form a new binder or base course.
To recycle the surface layer and a few centimeters of the course of semi rigid pavement in order to restore the bonding and to reconstitute a new surfacing.
To recycle alone the bituminous wearing course to remedy surface layer problem such as cracking, excessive ageing of binder, etc.

## Slide 7: Cold in-situ recycling Limits of use
Climatic condition too low
Max size < 80mm
Presence of geo textile
Presence of many services exits and manholes
Homogeneity of the old pavement

## Slide 8: State of the art: French guide

## Slide 9: Objectives and Classification
Type | Emulsion |  |  | Cement
Class | 1 | 2 | 3 | 4
Goal | Structural Reinforcement | Wearing course rehabilitation | Wearing course rehabilitation | Structural reinforcement
Existing pavement | Few cm of AC + unbound or bound base course | 4 to 8 cm of AC + unbound or bound base course | 100% of AC | AC + binder and base course
Use | Base course | Binder course | Binder course | Base course

## Slide 10: Objectives and Classification
Type | Emulsion |  |  | Cement
Class | 1 | 2 | 3 | 4
Goal | Structural Reinforcement | Wearing course rehabilitation | Wearing course rehabilitation | Structural reinforcement
Use | Base course | Binder course | Binder course | Base course
Binder | Emulsion | Rejuvenating emulsion | Rejuvenating emulsion | Cement or similar
Binder content | 3 to 5 % residual binder | 1 to 3 % residual binder | Up to 2 % residual binder | 3 to 7 % hydraulic binder
Thickness | 10 to 15 cm | 5 to 12 cm | 5 to 12 cm | 20 to 30 cm

## Slide 11: Cold in-situ recycling Mechanical performances
Results of Duriez test | Modulus at 15° C (MPa)
Unbound graded aggregate stabilized with emulsion (class 1): R at 14 days between 1.5 and 2.2 MPa and r/R > 0.55 R at 14 days between 2.2 and 3.3MPa and r/R > 0.55 | 1500 2500
Recycled material with emulsion including 75 to 90% of reclaimed bituminous material (class 2): R at 14 days lower than 4MPa and r/R > 0.65 R at 14 days higher than 4 MPa and r/R > 0.65 | 2000 3000
Recycled material with emulsion with more than 90% of reclaimed bituminous material (class 3): R at 14 days higher than 4 MPa and r/R >0.70 Other cases | 4000 3000
Correlation used in France between Duriez test results and estimated stiffness modulus

## Slide 12: Novacol Cold in-situ recycling Preliminary studies
Field investigation (boring, deflection, visual aspect)
Characterization of the in situ materials
Feasibility of in situ recycling
  Maximum size material
  Old binder characteristics (Pen-R&B)

## Slide 13: Novacol Cold in-situ recycling Mix design
Characterization of the material
Selection of the new binder to determine the need of rejuvenation
Binder determination according to the in situ total Asphalt concrete
  Class I : 3 to 5 %
  Class II : 1 to 3 %
  Class III : Up to 2%
Mechanical properties: water resistance (Duriez) & Gyratory Shear Press tests (PCG)

## Slide 14
TEST | BEFORE | AFTER
Pen at 25 °C (0,1 mm) | 5 - 11 | 15 - 22
R&B (°C) | 80 - 92 | 62 - 84
REJUVENATION AGEING BINDER
Target : R&B decrease from 5 to 15° C
Novacol Cold in-situ recycling

## Slide 15: Wearing course In situ treatment
In situ recycling as binder course
Sealing coat after compaction
Wearing course is adapted to the traffic:
  Surface dressing
  Micro surfacing,
  Thin AC
  Thick AC for Heavy traffic

## Slide 16: In situ recycling as wearing course
Depth from 5 to 7 cm thick
Calibrated reclaimed asphalt (milling procedure and old wearing course quality)
Special emulsion for a good coating and for rejuvenating the old binder
Binder | Before | After | Gain
Pen | 12 | 41 | 29
R&B | 70 | 56 | 14
Fraass | -2 | -11 | 9

## Slide 17: In situ recycling as wearing course
 | 1 month | 1 year | 3 years
Pen in 1/10mm | 32 | 33 | 32
R&B in °C | 61 | 57 | 60
Fraass point in °C | -11 | -9 | -8
Density in % | 87 | 88 | 87
Stiffness in MPa | 900 | 3200 | 3000
Texture depth in mm | > 0.6 | > 0.5 | > 0.4
Mechanical characteristic evolution

## Slide 18: Novacol Cold in-situ recycling
Perfect bonding
BEFORE
AFTER

## Slide 19
Before
During
19
After

## Slide 20: Novacol Cold in situ recycling
Very good bonding
Limoges airport
13 cm
NOVACOL
18 cm Cement material
5 cm AC
AC with asbestos
6 cm
AC
20 cm Cement material

## Slide 21
Structure in place:
  5 cm surface course
  6 cm Binder Course (AC)
The job :
  In situ recycling: 8 cm depth
  Rejuvenating emulsion: 2%
  Wearing course : thin asphalt concrete (Ruflex) 4 cm
Novacol typical job site in France
21

## Slide 22
Works under traffic

## Slide 23: In situ multi recycling
Traffic: 150 < HGV < 300
Pavement reinforced in 2001 with:
  4 cm thin AC
  8 cm of in situ cold recycling with emulsion
Asphalt concrete
Unbound materials
23

## Slide 24: 2010 maintenance
1st section
in situ treatment: 8 cm thick
micro surfacing
2nd section
milling of the existing wearing course
In situ treatment: 8cm thick
4 cm thin AC

## Slide 25: Binder characteristics
1st section: 100% of reclaimed asphalt with 2% special emulsion
2nd section: as above
 | Pen | R&B | Fraass
before | 7 | 75 | 7
after | 35 | 60 | -12
 | Pen | R&B | Fraass
before | 17 | 64 | -4
after | 38 | 53 | -11

## Slide 26: Special emulsion
 |  | Before | After | Gain
Traditional emulsion | Pen | 23 | 26 | 3
 | R&B | 62 | 58 | 4
 | Fraass | -7 | -11 | 4
Special emulsion | Pen | 12 | 41 | 29
 | R&B | 70 | 56 | 14
 | Fraass | 1 | -11 | 12

## Slide 27: Follow-up
All cores are stuck
Density:
  Traditional emulsion : 82-85%
  Special emulsion : 88-92%

## Slide 28
RN 10 slow lane : 20,000 vehicles / day, 16 % of HGV
after 10 years : no transversal deformation
Very high rutting resistance Transversal profile
28

## Slide 29
Life cycle analysis: energy consumption for 1 m² recycled road
29

## Slide 30
Life cycle analysis : GHG Emission for 1 m² recycled pavement
30

## Slide 31
31

## Slide 32: Very thin asphalt concrete BBTM
European standard 13108-2
Thickness from 20 to 30 mm
Aggregates: LA20-MDE15-PSV 50
Grading 0/6 and 0/10
Modified bitumen
Water resistance
2 classes
  Class 1: void content 12/19%
  Class 2: void content 20/25%
Mechanical stability (rutting test)

## Slide 33: French formulations
33

## Slide 34: BBTM uses
Main use
  High level of skid resistance
  Low rolling noise
Macro texture (Mean texture depth)
  BBTM 0/6: 0.7 mm for 90%
  BBTM 0/10: 0.9 mm for 90%
34

## Slide 35
40 60 80 100 120
0,70
0,60
0,50
0,40
0,30
0,20
0,10
9th decile
1st decile
0,00
Speed in km/h
BBTM
Longitudinal braking force coefficient

## Slide 36: BBTM uses
Existing pavement
  Take care about the support
  Tack coat to water proof the existing pavement
New pavement
  Binder course
  Take coat
36

## Slide 37: Novacol Cold in-situ recycling Advantages
To save new material by the re-use of whole in place
To reduce the energy consumption
To reduce the need for transport
To limit the ancillary works (adjustment of levels, raising kerbs)
Very economic about 30% less traditional techniques
Environmental less G.E.S.
To reopen the roadway to traffic immediately
To recycle only one lane if necessary
Etc…
37

## Slide 38: Conclusions
Cold in situ recycling
More than 25 years of knowledge
In situ recycling for the 2nd time
Good performances
Mechanical performance improvement
Environmental friendly technique
According to the treatment: No need of wearing course

## Slide 39: Conclusions
Very thin asphalt concrete
New wearing course
Good surface characteristics (noise, skid resistance, macro texture)
Check the existing wearing course before (cracks, transversal profiles, etc.)
Take coat !!!

## Slide 40
Thank you for your attention
40